## Slide 2
Should I talk about wall relaxation and seop theory at all?

## Slide 3: Outline
Form factor studies at Jefferson National Accelerator Facility
Spin-exchange optical pumping (SEOP)
3He polarimetry
Development of hybrid cells
Polarized 3He target cells incorporating metal

## Slide 4: Elastic form factor of neutron
The Fourier transform of elastic form factor provides information of the charge distribution inside neutron.
Core is positive and “proton like”
Core is surrounded by negative pion cloud

## Slide 5: 3He Target for studying neutron
Free neutrons are unstable, they decay in less than 15 minutes
To first order approximation, a 3He nucleus has two protons with paired spins, and a single neutron that accounts for most of the nuclear spin.
Notes: Some notes

## Slide 6: Effective luminosity
In a double-spin asymmetry experiment, the measured asymmetry is
where
with L and t being luminosity and experiment duration, respectively
Effective luminosity
Notes: Double-spin: polarized electrons are scattered of off polarized 3He atoms
N: the number of detected events
Ibeam: electron beam current
e: the charge of the electron
[He]: He density
l: length of the target chamber

## Slide 7: The performance of polarized 3He targets have increased by a factor of 30 since slac e142
Demonstrated by simulated beam test

## Slide 8: Traditional 3He target cell
Transfer Tube
Forced-Air Oven

## Slide 9: SPIN-exchange optical pumping (seop)

## Slide 10: 3He spin Relaxation
The total relaxation of 3He nucleus spin polarization due to all processes except for spin exchange:
Dipolar relaxation rate at 23C
Static field inhomogeneity
Wall relaxation
Notes: D: diffusion constant, \nablaBx and \nablaBy are the transverse magnetic field inhomogeneities, B0 is the holding field
\rho is the so-called relaxivity, S/V: surface to volume ratio

## Slide 11: X Factor
E. Babcock et al. reported evidence of a previously unrecognized spin relaxation mechanism (leave citation here?):
With infinite laser power
More on this later.
Notes: X appears to be temperature dependent and rougly proportional to alkali density. X limits the maximally achievable 3He polarization even with infinite laser power.

## Slide 12
Helmholtz Coil
Oven
Target Cell
z
x
y
Holding Field:
RF field:
RF Coil
In rotating frame:
Adiabatic fast passage (afp)

## Slide 13: Adiabatic fast passage
During a field-sweeping AFP measurement

## Slide 14: AFP losses
Longitudinal spin-relaxation rate on resonance
Fractional relaxation due to a single AFP flip
Measurements and theory agree extremely well

## Slide 15: Pulsed nuclear magnetic resonance (pnmr)
A short pulse of RF field is applied on a small region of the target
The frequency of the pulse is equal to the Larmor frequency, so in the rotating frame
A typical free induction decay (FID) is shown below:

## Slide 16: Electron paramagnetic resonance (epr)
The shift of Zeeman splitting of alkali metal is largely caused by Fermi-contact interaction
The effective field causing the shift is produced by polarized 3He multiplied by an enhancement factor
By flipping 3He spins, we can isolate the effective field from holding field and other ambient fields
Thus 3He polarization can be calculated using the frequency shift

## Slide 17: Spinup
Time evolution of polarization in a double-chambered cell:
Notes: 3 parameter fit is done with equation for single-chambered target cell
Y axis is polarization because the AFP signals have been calibrated with EPR

## Slide 18: spindown
Exponential decay of nuclear polarization:
T1 is the so-called life time.
A spindown curve at room temperature
Notes: Y axis is raw amplitudes from AFP measurements.

## Slide 19: Initial spinup
By performing a Taylor expansion on the time evolution of polarization:

## Slide 20: The k-3he spin-exchange rate constant
The quantity mpc can also be measured with a technique based on Faraday rotation
Both mpc values should agree, fitting the ratio to one gives

## Slide 21: Maximum achievable 3He polarization
The so-called X factor characterizes a poorly understood temperature-dependent spin-relaxation mechanism that limits the maximum polarization
The relaxation mechanism described by the X factor has been observed to be roughly proportional to the spin-exchange rate, so it cannot be overwhelmed with infinite laser power.
Babcock, Chann, Walker, Chen and Gentile
PRL vol. 96, pg. 083003 (2006)

## Slide 22: The x factor hot relaxation method
“The hot relaxation method” is a method of measuring the X factor by looking at spin-relaxation rates at different temperatures [1].
[1]E. Babcock, B. Chann, T. G. Walker, W. C. Chen, and T. R. Gentile, Phys. Rev. Lett. 96, 083003 (2006).
Measured with spinups and cold spindowns.
Determined with measured alkali densities and known spin-exchange coefficients

## Slide 23: The x factor Single temperature methods
X factor can also be determined with data from a single temperature using various methods.

## Slide 24: Errors and weighted average
Error for each determination of X:
To combine different determinations of X, a weighted average was obtained for which the weights are varied until the combined error is minimized

## Slide 25: Possible temperature dependence
Our evidence suggests there may be temperature dependence in the X factor.

## Slide 26: Metal end windows
Maximum beam current used during the 6 GeV era at JLab was 15 μA.
Future experiments during the 12 GeV era planned to use up to 60 μA.
Glass windows are not likely to survive currents above 30 μA.
Thus higher luminosity experiments require the development of metal end windows for spin-exchange polarized 3He cells.
Results from Mainz show ~20 hr spin-relaxation time for 3He targets with gold incorporated
Mainz tests did NOT involve alkali metals
Notes: Mainz used metastability-exchange polarized 3He

## Slide 27: Mainz results
Gold measured at 20 hours, which should be more than enough.

## Slide 28: New cell design with metal end windows

## Slide 29: Metal cell fabrication
Houskeeper seals by Larson
Glass-metal-glass seals made by Larson Electronic Glass
Mechanically polished by our machine shop
Electropolished by Able Electropolishing
Electroplated by Epner Technology Inc.
Cleaned with our ultrasonic cleaner
Made into test cells by Mike Souza
Filled to 1atm (3He + N2)
Gold coated tube (left) vs. bare oxygen-free high thermal conductivity (OFHC) copper tube (right)

## Slide 30: METAL CELLS WITH OFHC COPPER
Spool piece
Goldfinger
Cupid
Gold Rush
GoldenEye
GoldenVec 1
GoldenVec 2

## Slide 31: Cells with other materials
Pyrah
(Control Cell)
TitanVec
Titan

## Slide 32: Experimental setup: Optics
3He test cell polarized using SEOP
Oven heated to 170oC
Laser and holding field
Hand-wrapped pick up coil

## Slide 33: Experimental setup: Gradient coils
The orientations of the three sets of gradients coils are chosen such that each of them controls one component of the holding field gradients.
The gradient tensor at the center is:
The last column is the most important.

## Slide 34: Magic angle
Magic angle: Θm=cos-11/√3=54.7o
With theses angles, each set of gradient coils has one nonzero value in the third column.
The gradient coils are critical for obtaining FID signals with long transverse relaxation time and high signal-to-noise.

## Slide 35: Experimental setup: PNMR setup
The pickup coil was lower than the center of the field
Settings of gradient coils require tweaking

## Slide 36: Spindowns with multiple sampling rates
3 Spindowns of GoldenVec1 each with a different sampling rate:

## Slide 37: Extracting true lifetime
Linear fit of the three lifetimes to extract corrected lifetime and PNMR loss

## Slide 38: Relaxation measurement results: tyrion
Tyrion was a spherical GE180 cell with gold coated on the interior surface.
Measured lifetime was 1.21 hr.
The short lifetime was attributed to impurities in the cell.
All other techniques explored to coat gold on glass directly were difficult.
Next step was to investigate gold coating on metal and bond the metal piece to glass.

## Slide 39: Relaxation measurement results: SPOOL PIECE
First cell with OFHC copper.
The OFHC copper tube was attached to a glass flange with o-rings for making the seal.
The 2.14 hr lifetime was attributed to outgassing from o-rings.
The lifetime of the separated PC was 109.2 hr.
New ways to bond metal to glass should be investigated.

## Slide 40: Vertical metal cells: goldfinger and cupid
All glass-metal seals from this point on were made with Houskeeper seal by Larson Electronic Glass.
First two cells showed degradation of lifetime.
Cupid degraded from 3.6 hr to 2.4 hr
Goldfinger degraded from 2.8 hr to 0.3 hr
Rb forms almal gam with metal
Notes: Explain what I mean by vertical metal cells

## Slide 41: Vertical metal cells: goldrush
Our first gold coated cell with more than 10 hr lifetime.

## Slide 42: Effects of field inhomogeneities
The lifetime increased from roughly12 hr to 14.81 hr after elevated by 10 cm.

## Slide 43: pure pyrex control cell: pyrah
Goldrush after elevation:
14.81 hr
Pyrah after elevation:
26.5 hr

## Slide 44: Horizontal cells: goldenvec
Design of horizontal cell:
Goldenvec had a lifetime of 10.6 hr.
Overall vertical length reduced from 15.75’’ to roughly 10’’.

## Slide 45: goldenvec2
Same design as Goldenvec.
Filled with cryogenic trap instead of noble gas purifier because of the success with Protovec2.
Lifetime increased to 15.6 hr, longest we have to date.
All metal cells afterwards were filled with cryogenic trap.

## Slide 46: Ge180 cells: goldenvec180 and goldenvec360
It was widely acknowledged that GE180 had less wall relaxation compared to Pyrex.
Goldenvec180 and Goldenvec360 followed the same design as Goldenvec.
Corning 7052 was used as the transition glass to bond OFHC copper to GE180.
Measured lifetime was 4.43 hr for Goldenvec180 and 3.01 hr for Goldenvec360.
Was it the transition glass, the melt of GE180 or insufficient annealing?

## Slide 47: Test on transition glass
Two test cells were made with canary glass (uranium glass) because of our previous experience with it.
One cell had vertical configuration with Pyrex and one had horizontal configuration with GE180.
Pyrex cell had 22.7 hr lifetime even though uranium is paramagnetic.
GE180 cell was prepared the same way as Goldenvec2 and had 6.39 hr lifetime without metal.
Problem is likely to be directly related to GE180 itself!
Notes: Uranium is paramagnetic, but gave long enough lifetime.

## Slide 48: The glass or the annealing
A spherical GE180 cell was made.
The measured lifetime was 72 hr.
The glass directly attached to metal was not placed in oven for annealing.
Spliced to the cell after the rest of the cell was baked.

## Slide 49: Goldfinger180
A GE180 with vertical configuration was made.
The glassblower minimized the amount of glass that was not placed in oven.
The top Houskeeper seal was leaking. The epoxy type sealant Stycast 1266 was used to fix it.
The lifetime was 10.4 hr before elevation, and 12.4 hr after elevation.
Metal end windows are predicted to contribute less than 1/100 hr-1 relaxation rate.
Proper annealing is very important!

## Slide 50: Pyrex cells with titanium
Titan was a Pyrex cell with titanium tube and vertical configuration.
Its lifetime was so short that no spindown was obtained.

## Slide 51: Pyrex cells with titanium
Titanvec was a horizontal Pyrex cell with gold-coated titanium tube.
Gold started to peel off of titanium tube during ultrasonic cleaning.
The measured lifetime was 0.52 hr.

## Slide 52: Thank you!

## Slide 53: Backup slides metal cell table

## Slide 54: backup slides metal cell table

## Slide 55: Backup slide metal cell lifetime table

## Slide 56: Backup slides cryogenic trap